Consider the following paragraph into all Division 8 sections that will require a transition. Part 2 Products, as an accessory

Perimeter Seal to Windows, Doors, Curtainwall and Storefront Systems: Provide Proglaze Engineered Transition Assembly (ETA), manufactured by Tremco, Inc evaluated in accordance with the following properties:

ASTM E 283 Test Method for Determining Rate of Airflow Through Exterior Windows, Curtain Walls and Doors Under Specified Pressure Differences Across the Specimen.

ASTM E 330 Test Method for Structural Performance of Exterior Windows, Curtain Wall and Doors by Uniform Static Air Pressure Differential

ASTM E 331 Test Method for Water Penetration of Exterior Windows, Curtain Walls and Doors by Uniform Static Air pressure Difference.

ASTM E 547 Test Method for Water penetration of Exterior Windows, Curtain walls and Doors by Cyclic Static Air Pressure Difference

Products:

Pre-engineered, silicone extrusion, with integral dart and/or single or double rib extruded sheet. The system assembly is adhesively sealed with Spectrem( 1 to the window assembly to provide an airtight and waterproof seal to the structure. The engineered transitions assembly maybe comprised of the following components;

- Silicone Rubber Sheet (SRS): Extruded, 40 durometer, ribbed

- translucent silicone sheet.

- Silicone Transition Profiles:  Three dimensional injected molded profiles should be used where appropriate.

- Silicone Rubber Extrusion (SRE) Extruded, 40 durometer translucent silicone with lock-in dart.

- Metal adaptor to accept Silicone Rubber Extrusion.

- Silicone Sealants: Comply with ASTM C920, single-component, neutral-curing silicone; Class 100/50, Grade NS, Use O. Product shall be:  Spectrem( 1 as manufactured by Tremco.